| 塑料用热塑性丙烯酸树脂Thermoplastic Resin |
| --- |
| 产品型号 Product Code | 固含 Non-volatile | 粘度 Viscosity | 色数 Color | 酸价 Acid Value | Tg | 溶剂 Solvent | 特性 Properties | 用途 Application |
| PJ8040A | (50±2)% | (8-15)s(格/25℃) (8-15)s（Garden/25℃) | ≤1# | ≤4mgKOH/g | 34℃ | 甲苯 TOL | 耐候,柔韧性优,光泽高,保光性好 Good weathering resistance,excellent flexibility,high gloss,good gloss stability. | 罩光清漆,塑料漆,硝基清漆 Varnish,plastic coating,NC lacquer. |
| PJ8040B | (55±2)% | (50-75)s(格/25℃) (50-75)s（Garden/25℃) | ≤1# | ≤15mgKOH/g | 36℃ | 二甲苯 XYL | 附着力好，耐化学品性好，保光保色性好 Good adhesion and chemical resistance, good gloss and color stability. | 油性外墙涂料、混凝土密封底漆 External wall coating,concrete sealer. |
| PJ8040C | (60±2)% | (80-150)s(格/25℃) (80-150)s（Garden/25℃) | ≤1# | ≤6mgKOH/g | 60℃ | 甲苯 TOL | 耐候,硬度高,光泽高,保光性好,与CAB相容佳 Good weathering resistance,high hardness,gloss stability,good compatibility with CAB. | 罩光清漆,塑料漆,硝基清漆 Varnish,plastic coating,NC lacquer. |
| PJ8040D | (50±2)% | (60-80)s(格/25℃) (60-80)s（Garden/25℃) | ≤1# | ≤6mgKOH/g | 80℃ | 甲苯 TOL | 干燥快,硬度高,流平性好,保光性好,与CAB相容性佳 Fast drying,high hardness,good levelling,,gloss stability,good compatibility with CAB. | 塑胶漆,马路划线漆,木器漆 Plastic coating,road marking paint,wood paint. |
| PJ6001-45 | (45±2)% | (20-60)s(格/25℃) (20-60)s（Garden/25℃) | ≤1# | ≤5mgKOH/g | 90℃ | 甲苯、异丁醇、乙酯 TOL、IBA、EAC | 附着力好，与CAB、NC的相溶性佳，耐醇性、耐化学品性好 Good adhesion,excellent compatibility with CAB and NC,good alcohol and chemical resistance. | 塑料金属漆、实色漆 Plastic silver paint,enamel. |
| PJ6019-50 | (50±2)% | (150-210)s(格/25℃) (150-210)s（Garden/25℃) | ≤1# | ≤1mgKOH/g | 88℃ | 甲苯、异丁醇、丁酯 TOL、IBA、BAC | 与CAB、NC混溶性好，硬度高，铝粉排列性优，耐醇、耐水煮性好，与UV面漆附着力好 Good compatibility with CAB and NC,high hardness,good metallic effect,alcohol resistance,boiling resistance,excellent adhesion to UV top coat. | 塑胶底漆、铝粉漆 Plastic base coat,silver paint. |