| 聚酯树脂Saturated Polyester Resin |
| --- |
| 产品型号 Product Code | 固体份 Non-volatile | 粘度 Viscosity | 色数 Color | 酸价 Acid Value | 羟值 OH Value | 溶剂 Solvent | 特性 Properties | 用途 Application |
| PJ315 | (72±2)% | (13-35)s(格/25℃) (13-35)s（Garden/25℃) | ≤1# | ≤12mgKOH/g | — | 二甲苯、重芳烃 XYL、Solvesso100 | 高固低粘，耐候性好，保光保色性好 High solidity,low viscosity,good weathering resistance,excellent gloss and color maintenance. | 高丰满度、高鲜映性烤漆 High fullness and high DOI baking coat. |
| PJ352-60 | (60±2)% | (45-80)s(格/25℃) (45-80)s（Garden/25℃) | ≤1# | ≤5mgKOH/g | — | 二甲苯、重芳烃 XYL、Solvesso100 | 经济型产品，硬度高，柔韧性好。 Economic type product,high hardness,good flexibility | 高硬度氨基烘漆,卷材涂料 High hardness amino baking coat,coil coating. |
| PJ320 | (60±2)% | (4-15)s(格/25℃) (4-15)s（Garden/25℃) | ≤1# | ≤10mgKOH/g | 60±10 | 二甲苯 XYL | 硬度高,耐候,抗冲击、重涂性好 High hardness,good impact resistance,excellent recoatability,good weathering resistance. | 高硬度氨基烘漆,汽车中涂漆,金属底色漆,卷钢涂料 High hardness amino baking coat,automotive mid & top coating,coil coating. |
| PJ340 | (70±2)% | (5-15)s(格/25℃) (60%) (5-15)s（Garden/25℃) (60%) | ≤1# | ≤15mgKOH/g | 70±10 | 二甲苯 XYL | 色数浅,漆膜硬度高,耐冲击,耐候性,耐化学品性,抗黄变优异 Light color,good chemical resistance,high hardness,good weathering resistance,anti-yellowing. | 高硬度氨基烘漆,汽车中涂漆,金属底色漆,卷钢涂料 High hardness amino baking coat,automotive mid & top coating,coil coating. |
| PJ330-70 | (70±2)% | (5-12)s(格/25℃) (5-12)s（Garden/25℃) | ≤1# | ≤15mgKOH/g | 120±20 | 二甲苯 XYL | 柔韧性好,耐深冲性佳,光泽高,耐候,多种树脂相容好 Good flexibility,good deep drawing resistance,high gloss,good weathering resistance,excellent compatibility with other resins. | 高丰满度PU漆、烤漆,色浆基料或用于调整产品的柔韧性 High fullness PU coating,baking coat,pigment paste,improving flexibility. |
| PJ350 | (60±1)% | (25-50)s(格/25℃) (25-50)s（Garden/25℃) | ≤2# | ≤12mgKOH/g | — | 二甲苯、重芳烃 XYL、Solvesso100 | 耐深冲性,耐化学品性,硬度高,耐候性,耐黄变 Good flexibility,good deep drawing resistance,anti-yellowing ,good weathering and chemical resistance,high hardness. | 卷钢,制罐涂料、印铁油墨 Coil coating,can coating,ink. |
| PJ360 | (70±2)% | (3-10)s(格/25℃) (3-10)s（Garden/25℃) | ≤1# | ≤15mgKOH/g | — | 二甲苯 XYL | 色数浅,耐化学品性好,硬度高,耐候性,抗黄变,相溶性好 Light color,good chemical resistance,high hardness,good weathering resistance,anti-yellowing,good compatibility. | 各类聚酯氨基清烘漆、色漆，色浆基料 Polyester-amino baking coating,pigment paste. |
| PJ390 | (60±2)% | (15-30)s(格/25℃) (15-30)s（Garden/25℃) | ≤1# | ≤12mgKOH/g | 80±10 | 二甲苯、重芳烃 XYL、Solvesso100 | 附着力好,抗冲击,硬度高,耐黄变性佳 Good adhesion,anti-impact,high hardness,anti-yellowing resistance. | 汽车金属色底漆、实色面漆、中涂漆 Automotive base & top coat,mid coating. |