| 改性醇酸树脂Modified Alkyd Resin |
| --- |
| 产品型号 Product Code | 改性方式 Modified Type | 固体份 Non-volatile | 粘度 Viscosity | 色数 Color | 酸价 Acid Value | 溶剂 Solvent | 特性 Properties | 用途 Application |
| PJ14-70 | 苯乙烯 Styrene | (70±2)% | (30-100)s(格/25℃)(60%) (30-100)s（Garden/25℃) (60%) | ≤8# | ≤12mgKOH/g | 二甲苯、松节水 XYL、Turpentine | 粘度高,干燥快 High viscosity,fast drying. | 金属锤纹漆,快干底漆,磁漆,绝缘漆 Metal hammer paint,fast drying base coat,enamel,insulating varnish. |
| PJ17-60B | 丙烯酸 Acrylate | (60±2)% | (25-80)s(格/25℃) (25-80)s(Garden/25℃) | ≤7# | ≤10mgKOH/g | 二甲苯、松节水 XYL、Turpentine | 耐候,抗黄变,表干快,柔韧性好 Good weathering resistance,anti-yellowing,fast drying,good flexibility. | 机车修补漆,户外钢结构、电线杆涂料 Automotive refinish,outdoor structural steel paint,telegraph pole coating. |
| PJ3605A | TDI | (55±2)% | (60-140)s(格/25℃) (60-140)s(Garden/25℃) | ≤6# | ≤5mgKOH/g | D40 | 附着力优,耐水性好,干性快,硬度高,耐磨 Good adhesion and water resistance,fast drying,high hardness,good abrasion resistance. | 磁漆,绝缘漆,防腐漆 Enamel,insulating varnish,anticorrosive paint. |
| PJ4605 | TDI | (55±2)% | (15-40)s(格/25℃) (15-40)s(Garden/25℃) | ≤10# | ≤6mgKOH/g | 二甲苯、汽油 XYL、M.S | 颜料分散,附着力佳 Good pigment wetting and adhesion. | 真空电镀底油,1KPU磁漆，防腐漆 Vacuum metalizing base coat,1KPU enamel,anticorrosive paint. |
| PJ4606 | TDI | (55±2)% | (20-70)s(格/25℃) (20-70)s(Garden/25℃) | ≤8# | ≤6mgKOH/g | 汽油 M.S. | 颜料分散,附着力佳,硬度高,抗冲击 Good pigment wetting and adhesion,high hardness,good impact resistance. | 真空电镀底油,单组份PU漆 Vacuum metalizing base coat,1KPU paint. |
| PJ4606A-1 | TDI | (55±2)% | (10-25)s(格/25℃) (10-25)s(Garden/25℃) | ≤8# | ≤6mgKOH/g | 200#汽油 | 快干，粘度低,光泽高，附着力好 Fast drying,low viscosity,high gloss,good adhesion. | 真空电镀底油,单组份PU漆 Vacuum metalizing base coat,1KPU paint. |
| PJ4605(B类) | TDI | (55±2)% | (2500-4000)mPa.s | ≤10# | ≤6mgKOH/g | D40 | 环保型PJ4605 Environmental PJ4605 | 真空电镀底油,单组份PU漆 Vacuum metalizing base coat,1KPU paint. |
| PJ9103 | 丙烯酸 Acrylate | (70±2)% | (8-20)s(格/25℃)(60%) (8-20)s(Garden/25℃)(60%) | ≤12# | ≤15mgKOH/g | 甲苯、二甲苯 TOL、XYL | 干燥快，易起皱 Fast drying,easy forming wrinkle. | 真空电镀底油,皱纹漆 Vacuum metalizing base coat,wrinkle paint. |