| 工业用醇酸树脂Alkyd Resin For Industry Paint |
| --- |
| 产品型号 Product Code | 油类 Oil Type | 油度 Oil length | 固体份 Non-volatile | 粘度 Viscosity | 色数 Color | 酸价 Acid Value | 主要溶剂 Solvent | 特性 Properties | 用途 Application |
| PJ11-70CA | 脂肪酸 Fatty acid | 短 Short | (70±2)% | (30000-50000) mPa.s/25℃ | ≤2# | ≤12mgKOH/g (60%) | 二甲苯 XYL | 色数浅,硬度高,快干,光泽高 Light color,high hardness,fast drying,high gloss. | 快干氨基烤漆,硝基漆 Fast drying amino baking coat,NC lacquer. |
| PJ11-70DA | 脂肪酸 Fatty acid | 短 Short | (70±2)% | (70000-120000) mPa.s/25℃ | ≤2# | ≤12mgKOH/g (60%) | 甲苯、二甲苯 TOL、XYL | 粘度高,硬度高,超快干 High viscosity,high hardness,fast drying. | 超快干氨基漆,硝基漆，银粉漆 Fast drying amino baking coat,NC lacquer,silver paint. |
| PJ12-70A | 椰子油脂肪酸 Coconut fatty acid | 短 Short | (70±2)% | (20000-40000) mPa.s/25℃ | ≤1# | ≤12mgKOH/g (60%) | 二甲苯 XYL | 色数浅,光泽高,硬度好,耐黄变 Light color,high hardness,high gloss,anti-yellowing. | 耐黄变快干氨基烤漆,硝基漆 Fast drying anti-yellowing baking coat,NC lacquer. |
| PJ3346 | 大豆油 Soya bean oil | 短 Short | (60±2)% | (10-20)s(格/50%) (10-20)s(Garden/50%) | ≤6# | ≤12mgKOH/g | 二甲苯 XYL | 光泽高,柔韧性好,硬度高，干燥快 High gloss,good flexibility,high hardness,fast drying. | 高光泽氨基烤漆 High gloss amino baking coat. |
| PJ3438 | 大豆油 Soya bean oil | 中 Medium | (78±2)% | (15-40)s(格/50%) (15-40)s(Garden/50%) | ≤6# | ≤15mgKOH/g | 二甲苯 XYL | 高固低粘，丰满度好，光泽高 High solidity,low viscosity,high gloss. | 高光泽氨基烤漆 High gloss amino baking coat. |
| PJ3616 | 大豆油酸 Soya fatty acid | 长 Long | (60±2)% | (80-200)s(格) (80-200)s(Garden) | ≤8# | ≤10mgKOH/g | 汽油 M.S. | 光泽高,柔韧性好,不易黄变 High gloss,good flexibility,anti-yellowing. | 醇酸清漆、磁漆、醇酸底漆 Alkyd air-drying varnish,enamel,base coat. |
| PJ3495 | 大豆油酸 Soya fatty acid | 中 Medium | (50±2)% | (15-50)s(格) (15-50)s(Garden) | ≤10# | ≤10mgKOH/g | 汽油 M.S. | 快干,丰满,光泽高 Fast drying,good fullness and high gloss. | 醇酸清漆,醇酸磁漆,醇酸底漆 Alkyd air-drying varnish,enamel,base coat. |
| PJ3497 | 大豆油酸 Soya fatty acid | 中 Medium | (75±2)% | (70000-90000) mPa.s/25℃ | ≤10# | ≤15mgKOH/g | 二甲苯、汽油 XYL、M.S. | 高固低粘，干燥快，光泽高 High solidity,low viscosity,high gloss. | 低VOC自干漆 Low VOC air-drying paint. |
| PJ3515-75 | 大豆油酸 Soya fatty acid | 中 Medium | (75±2)% | (30000-60000) mPa.s/25℃ | ≤10# | ≤15mgKOH/g | 二甲苯、汽油 XYL、M.S. | 高固低粘，干燥快，光泽高 High solidity,low viscosity,high gloss,fast drying. | 低VOC自干漆 Low VOC air-drying paint. |
| PJ6565 | 亚麻油 Linseed oil | 中 Medium | (52±2)% | (20-50)s(格) (20-50)s(Garden) | ≤10# | ≤20mgKOH/g | 汽油 M.S. | 干燥快，光泽高 Fast drying,high gloss. | 醇酸漆 Alkyd air-drying varnish,enamel,base coat. |