| UV树脂UV Oligomer |
| --- |
| 产品型号 Product Code | 类型 Type | 官能度 Functionality | 色数 Color | 粘度 Viscosity | 酸价 Acid Value | 有效成份 Effective Components | 特性 Properties | 建议用途 Application |
| PJ9816-1 | 纯丙烯酸 Full Acrylate | 2 | ≤1# | (20000-35000) mPa.s/25℃ | ≤5mgKOH/g | 85% | 在金属上有良好的附着力，反应性适中，收缩率低 Good adhesion on the metal,moderate reactivity,low shrinkage | 真空电镀面油，金属UV涂料 UV vacuum metalizing top coating,UV paint for metal |
| PJ9813 | 纯丙烯酸 Full Acrylate | 2 | ≤1# | (30000-70000) mPa.s/25℃ | ≤5mgKOH/g | 100% | 柔顺性、抗裂性好，附着力佳，优异的耐候性，可重涂 Good flexibility and adhesion,excellent cracking resistacne and weathering resistance,good recoatability. | 电动车UV涂料，油箱UV漆 UV paint for Motorcycle and its gasoline tank |
| PJ9826A-100 | 聚氨酯 Aliphatic Urethane Acrylate | 3 | ≤1# | (30000-50000) mPa.s/25℃ | ≤1mgKOH/g | 100% | 柔顺性好，低收缩，瞬间黄变性及耐候性优异，相溶性好 Good flexibility,low shrinkage,excellent weathering resistance,good compatibility. | 用于调整柔性和耐候性 Improve flexibility and weathering resistance |
| PJ9835-1 | 聚氨酯 Aliphatic Urethane Acrylate | 3 | ≤1# | (3000-9000) mPa.s/60℃ | ≤1mgKOH/g | 95% | 很好的柔韧性和弹性，附着力好，对镀层的吸附力好 Good flexibility and excellent adhesion with plated metal | 真空电镀底油，皮革装饰涂料 UV vacuum metalizing basecoat,UV paint for leather |
| PJ9851 | 聚酯 Polyester Acrylate | 2 | ≤1# | (50000-80000) mPa.s/25℃ | ≤15mgKOH/g | 100% | 润湿性好，柔顺性佳，流平、丰满度佳,抗划伤，耐冷热循环和耐水煮性能好 Good pigment wetting,good flexibility and levelling,excellent fullness and levelling,good scratch resistance,anti-cold-hot cycles resistance,boiling water resistance | 高档金属、塑料UV漆 High quality UV paint for metal and plastic |
| PJ9855 | 聚酯 Polyester Acrylate | 3 | ≤1# | (50000-80000) mPa.s/25℃ | ≤15mgKOH/g | 100% | 润湿性好，柔顺性佳，耐冷热循环和耐水煮性能好 Good pigment wetting,good flexibility ,Anti-cold-hot cycles resistance,boiling water resistance | UV油墨 UV ink |
| PJ9801A | 改性环氧 Modified Epoxy | 2 | ≤1# | (8000-12000) mPa.s/25℃ | ≤10mgKOH/g | 100% | 快干，润湿性好 Fast drying,good pigment wetting | 木器UV漆 UV paint for wood |
| PJ9802A | 双酚A环氧 Bisphenol A Epoxy | 2 | ≤1# | (1000-2500) mPa.s/60℃ | ≤5mgKOH/g | 100% | 固化快、流平好、硬度高 Fast cure,excellent levelling,high hardness | 塑料或木材UV漆 UV paint for wood or plastic |
| PJ9803A | 改性环氧 Modified Epoxy | 2 | ≤1# | (4000-7000) mPa.s/60℃ | ≤5mgKOH/g | 100% | 流平好，柔韧性好，收缩低 Excellent levelling,good flexibility,low shrinkage | 大面积喷涂UV漆 Large-area spray UV paint |
| PJ9806A | 改性环氧 Modified Epoxy | 2 | ≤1# | (10000-25000) mPa.s/25℃ | ≤5mgKOH/g | 100% | 润湿性好，柔顺性佳，在金属上有一定的附着力，对镀层有吸附力 Good pigment wetting and flexibility,good adhesion on metal,good adhesion with plated metal | 塑料、木材、金属UV漆、普通真空电镀底漆 UV coating for wood,plastic,metal,general vacuum metalizing basecoat |
| PJ9809A | 脂肪族环氧 Aliphatic Epoxy | 3 | ≤1# | (7000-15000) mPa.s/25℃ | ≤10mgKOH/g | 80% | 附着力优异，重涂性好，固化速度快，表面性能好 Excellent adhesion,good recoatability,fast cure. | UV真空电镀底油，可直接重涂UV漆 UV vacuum metalizing basecoat,UV recoatable paint |
| PJ9810A-60 | 纯丙烯酸 Full Acrylates | 2 | ≤1# | (500-800) mPa.s/25℃ | ≤10mgKOH/g | 60% | 流平好，反应速度快，光泽高，耐化学品性能好 Good levelling,fast cure,high gloss,good chemical resistance | 机壳罩光漆 UV varnish for mobile telephone & television shell,etc. |
| PJ9812-60 | 纯丙烯酸 Full Acrylates | 2 | ≤1# | (3000-6000) mPa.s/25℃ | ≤10mgKOH/g | 60% | 粘度适中，分子量大，耐磨性好，柔韧性佳 Moderate viscosity,high molecular weight,good abrasion resistance and flexibility | 机壳罩光漆 UV varnish for mobile telephone & television shell,etc. |
| PJ9815A-70 | 纯丙烯酸 Full Acrylates | 2 | ≤1# | (1000-2500) mPa.s/25℃ | ≤5mgKOH/g | 70% | 柔顺性好，附着力佳，重涂性好 Good flexibility and adhesion,excellent recoatability. | UV真空电镀底油，可直接重涂UV漆，烤漆的罩光清漆 UV vacuum metalizing basecoat,UV recoatable paint,UV varnish for baking basecoat |
| PJ9819 | 纯丙烯酸 Full Acrylate | — | ≤1# | (1500-2500) mPa.s/25℃ | ≤5mgKOH/g | 60% | 在金属上有良好的附着力，反应性适中，收缩率低 Good adhesion on the metal,moderate reactivity,low shrinkage | 真空电镀面油，金属UV涂料 UV vacuum metalizing top coating,UV paint for metal |
| PJ9820 | 聚氨酯 Aliphatic Urethane Acrylate | 6 | ≤1# | (3000-6000) mPa.s/60℃ | ≤2mgKOH/g | 100% | 反应速度快，高硬度，高耐磨，附着好 Fast cure,excellent abrasion resistance,high hardness,good adhesion. | 用于调整UV漆硬度、附着力及耐磨性 Improve hardness,adhesion,abrasion resistance |
| PJ9826A | 聚氨酯 Aliphatic Urethane Acrylate | 3 | ≤1# | (1000-2500) mPa.s/25℃ | ≤1mgKOH/g | 85% | 柔顺性好，低收缩，瞬间黄变性及耐候性优异，相溶性好 Good flexibility,low shrinkage,excellent weathering resistance,good compatibility. | 用于调整柔性和耐候性 Improve flexibility and weathering resistance |
| PJ9831 | 聚氨酯 Aliphatic Urethane Acrylate | 2 | ≤1# | (10000-20000) mPa.s/25℃ | ≤1mgKOH/g | 75% | 很好的柔韧性和弹性，附着力好，对镀层的吸附力好 Good flexibility and excellent adhesion with plated metal | 真空电镀底油，皮革装饰涂料 UV vacuum metalizing basecoat,UV paint for leather |
| PJ9832 | 聚氨酯 Aliphatic Urethane Acrylate | 3 | ≤1# | (10000-20000) mPa.s/25℃ | ≤1mgKOH/g | 90% | 很好的柔韧性，附着力好，对镀层的吸附力好 Good flexibility and excellent adhesion with plated metal | 真空电镀底油，皮革装饰涂料 UV vacuum metalizing basecoat,UV paint for leather |
| PJ9850 | 聚酯 Polyester Acrylate | 3 | ≤1# | (15000-35000) mPa.s/25℃ | ≤15mgKOH/g | 100% | 丰满度高，流平性好，柔顺性佳，耐冷热循环和耐水煮性能好 Good film builds,good flexibility and levelling,Anti-cold-hot cycles resistance,boiling water resistance | 高档金属、塑料UV漆 High quality UV paint for metal and plastic |
| PJ9851-1 | 聚酯 Polyester Acrylate | 3 | ≤1# | (20000-50000) mPa.s/25℃ | ≤10mgKOH/g | 100% | 低气味，低刺激性，对颜料的润湿性好,丰满度高，流平性好，柔顺性佳，耐冷热循环和耐水煮性能好 High viscosity，good pigment wetting,good film builds,good flexibility and levelling,Anti-cold-hot cycles resistance,boiling water resistance。Low irritation and low odour | 高档金属、塑料UV漆、UV油墨 High quality UV paint for metal and plastic，UV ink |
| PJ9851-2 | 聚酯 Polyester Acrylate | 3 | ≤1# | (4000-6000) mPa.s/25℃ | ≤10mgKOH/g | 100% | 粘度低,反应性适中,丰满度高，流平性好，柔顺性佳，耐冷热循环和耐水煮性能好 Good film builds,good flexibility ,Anti-cold-hot cycles resistance,boiling water resistance.Low viscosiry,moderate reactivity and good levelling | 高档金属、塑料UV漆,100%喷涂UV漆 High quality UV paint for metal and plastic,none-solvent-spraying UV coating. |
| PJ9801C | 改性环氧 Modified Epoxy | 2 | ≤1# | (5000-15000) mPa.s/25℃ | ≤10mgKOH/g | 100% | 快干，易打磨，润湿性好，附着力佳，性价比高 Fast drying,easy for sanding，good pigment wetting，excellent adhesion and more economical | 木器UV漆 UV primer or top coating for wood |
| PJ9804E | 改性环氧 Modified Epoxy | 2 | ≤1# | (40000-70000) mPa.s/25℃ | ≤3mgKOH/g | 100% | 反应性适中，流平、润湿性好，漆膜机械性能佳,施工性好,性价比高。 Moderate reactivity,excellent leveling，good pigment wetting，high hardness and good flexiblity, high quality and reasonable price | UV木器面漆、普通罩光漆 UV top coating for wood or common vanish |