| 金属制品/建筑用热塑性丙烯酸树脂Thermoplastic Acrylic Resin for Metal/Building |
| --- |
| 型号 Grade | 外观 Appearance | 固体份 Non-volatile | 粘度 Viscosity | 酸值 Acid Value | 色号Fe-co Color | 溶剂 Solvent | Tg | 突出特性 Outstanding Properties | 应用 Application |
| PJ60826-43 | 清澈透明 Clear | (43±2)% | (70-100)s(涂4/25℃) (70-100)s(Ford 4# cup/25℃) | (13-18)mgKOH/g | ≤1# | 甲苯 TOL | 25℃ | 与低分子环氧、NC混溶性、附着力优、有较快的干性 Compatibility with low molecular epoxy resin and NC ,adhesion, fast drying | 有色金属、真空电镀底面漆、玻璃自干漆 Nonferrous metals,vacuum plating primer-finish coat,glass air drying paint |
| PJ60827-43 | 清澈透明 Clear | (43±2)% | (50-90)s(涂4/25℃) (50-90)s(Ford 4# cup/25℃) | (10-19)mgKOH/g | ≤2# | 醋酸乙酯 EAC | 25℃ | 与低分子环氧、NC混溶性、附着力优、有较快的干性，微苯型 Compatibility with low molecular epoxy resin and NC ,adhesion, fast drying, micro-benzene conent |  |
| PJ60825-51 | 清澈透明 Clear | (51±2)% | (1-2)mPa.s/25℃ | (8-16)mgKOH/g | ≤2# | 醋酸乙酯/醋酸丁酯 EAC/BAC | 50℃ | 与低分子环氧、CAB混溶性、附着力优、硬度高、有较快的干性 Compatibility with low molecular epoxy resin and CAB ,adhesion, hardness, fast drying |  |
| PJ60034-50 | 清澈透明 Clear | (50±2)% | (6-13)mPa.s/25℃ | (5-10)mgKOH/g | ≤1# | 二甲苯/S-100溶剂油 XYL/S-100# | 34℃ | 光泽、快干性、优异的耐化学药品性、柔韧性和颜料润湿性 Gloss, fast drying, excellent chemical resistance, flexibility and pigment wetting | 水泥建筑内外墙漆 Cement building exterior paint |
| PJ60042-50 | 清澈透明 Clear | (49±2)% | (10-20)mPa.s/25℃ | (2-5)mgKOH/g | ≤2# | S-100溶剂油/200溶剂油 S-100#/200# | 42℃ | 环保性、低气味和优异的耐污性，快干性，柔韧性和颜料润湿性，施工性好 Environmentally, low odor and excellent stain resistance, fast drying, flexibility and pigment wetting, application property |  |
| PJ60053-50 | 清澈透明 Clear | (50±2)% | (10-16)mPa.s/25℃ | (5-9)mgKOH/g | ≤1# | 二甲苯/S-100溶剂油 XYL/S-100# | 53℃ | 光泽、快干性、优异的耐化学药品性 和颜料润湿性 Gloss, fast drying, chemical resistance and pigment wetting |  |